A comparison of chitin purification performance of an enzymatic process on four crustacean cuticles

Baron R.1, Rijba W.2, Socol M.1,4, Le Roux K.5, Bruzac S.1,6, Donnay-Moreno C.1, Cornet J.1, Ben Ismail H.2,3, Arhaliass A.7

1 Ifremer, Biorafhe, rue de l’Ile d’Yeu, BP 21105, 44311 Nantes cedex 03, France

2 Faculté des Sciences de Tunis, LR11ES09, Campus Universitaire El-Manar, 2092 El Manar Tunis, Tunisie. 3Institut National Agronomique de Tunis, 43 Avenue Charles Nicolle, 1082 Tunis, Mahrajène, Tunisie

4 present adress : LAAS CNRS, 7, avenue du Colonel Roche BP 54200 31031 Toulouse cedex 4, France

5 Ynsect, rue de l’Ile d’Yeu, BP 21105, 44311 Nantes cedex 03, France

6 present adress : Ifremer, LBCM, rue de l’Ile d’Yeu, BP 21105, 44311 Nantes cedex 03, France

7 Université de Nantes, GEPEA UMR CNRS 6144, CRTT, boulevard de l’Université, 44600 Saint-Nazaire cedex, France

A one-step bio-refinery process for crustacean cuticles was investigated. Its originality lies in a simple rapid (6 h) biotechnological cuticle fragmentation process that recovers all major compounds (chitins, peptides and minerals). The process consists of a controlled exogenous enzymatic proteolysis in a food-grade acidic medium allowing chitin purification (solid phase), and recovery of peptides and minerals (liquid phase).

This study is based on a comparison of four crustacean cuticles (shrimp Litopeneaus vannamei, lobster Homarus gammarus, invasive swimmer crab Polybius henslowii and invasive longnose spider crab Libinia dubia) on purity degree of chitin, on demineralization and deproteinization rates of solid phase after 6 h in presence of ASP enzyme at 40°C in formic acid diluted in 50 ml. An appropriate quantity of acid, depending on raw material mineral content, was added for each experiment for an initial dry weight of 5 g of raw material. Quantities of minerals and proteins of 5 g raw material were respectively 1.17 and 1.78 g for shrimp, 3.10 and 1.01 g for lobster, 3.11 and 0.96 g for swimmer crab and 3.54 and 0.29 g for spider crab. Final pH after 6 h were similar and between 3.4 and 3.6. In all cases, a similar demineralization rate after 6 h (between 96.7 % and 99.2 %) was observed. Best deproteinization rate (95.2%) was obtained for shrimp. At the opposite, 76.3 % was observed for spider crab. A dependence between deproteinization rate and ratio proteins on minerals of the raw materials seems to appear.

Objectif : Présentation orale flash (5mn) au congrès Oceanext Juin 2016.

Session 4 : Croissance bleue et valorisation des bio-ressources marines